# CONSANDTRATE

# Dry Crack Filler for concrete slabs

# Product Data Sheet

# Description: Water activated dry crack filler for concrete slabs.

# Use: ConSANDtrate Concrete Crack Filler is perfect for filling cracks and small holes in concrete and can also be used for a variety of uses. It's hard to fix a crack but its easy to fill a crack! When water freezes it expands so its best to fill any cracks or small holes in your driveway, sidewalks and patios.

# Application: install dry into cleaned crack. Spray with water until saturated thru.

# Test: LABORATORY REPORT / Report No. : 10101085-001-v1

Sample Description: Consandtrate Dry Crack Filler

Work requested: Compression testing per ASTM D695 and Freeze/Thaw test of supplied material

Test results relate only to the items tested. This document shall not be reproduced, except in full, without the written approval of Sherry Laboratories.The recording of false, fictitious, or fraudulent statements or entries on this document may be a punishable offense under federal and state law. A2LA

Accredited Laboratory Certificate No. 1089-01 (Mechanical) & 1089-02 (Chemical).

Compression Strength of Plastics per ASTM D695-10

Method of Preparing Specimens: Prepared per Clients Instructions

Specimen Type: Cylinder

Test Rate, in./min.: 0.05

Test Temperature, °F: 73°

Test Humidity, %: 29

S/N Diameter, in. Max. Load, lbs. Strength at Break, psi

C1 0.841 132.8 239

C2 0.839 169.3 306

C3 0.834 64.4 118

C4 0.842 287.1 516

C5* --- --- ---

Average --- --- 295

“Freeze/Thaw Test”

Test method was developed by the client to simulate the material being exposed to extreme environmental conditions. The sample was placed in a freezer for 72 hours at 0°F, allowed to warm to room temperature and examined under low magnification for and cracks or damages.

Results: No cracking or damage was observed.

# Packaging:

32 Oz. Plastic bottle / 12 units per box.

# Warranty: 30 days replacement.

ConSANDtrate, LLC

20111 A Mashburn Street

Pflugerville, Texas 78665

# www.ConSandtrate.com